| FLEXIBLE DISPLAY CENTER | Document Owner: Nick Munizza | Release Date: |
| --- | --- | --- |
| Document Title: DyMax 5000 UV Curing Flood Lamp Operating Procedure | Document No: | Document Rev: 01 |

| SIGNATURES FOR RELEASE OR HISTORY ON FILE IN PRODUCT SPECIFICATIONS | Confidential Proprietary |
| --- | --- |
| ORIGINATOR: Nick Munizza | The information contained in this document is the property of the Flexible Display Center at Arizona State University. No information contained in this document may be disclosed outside of the Flexible Electronics and Display Center at Arizona State University at any time. |
| RESPONSIBLE ENGINEER: Emmett Howard |  |
| DIRECTOR OF OPERATIONS: |  |  |

Table of Contents

1.0	Purpose	3

2.0	Scope	3

3.0	Associated Materials and Equipment	3

4.0	Safety 	3

5.0	Procedures	4

# Purpose

  - To define the operating procedures for the DYMAX model 38100 – 5000-EC UV Curing Flood Lamp system.

# Scope

  - The Dymax 5000-EC is a general-purpose UV light source with an effective curing area of approximately 5”x5”.

- Associated Materials and Equipment

  - Sample for curing.

- Safety

  - Approved Protective UV glasses / goggles.

- Procedures

  - Turn the unit on by press the power “ON” switch located on the left front of the power supply panel. The switch will light up to indicate that the power is ON.

  - After the lamp has ignited, allow 5 minutes for the lamp to reach its maximum output intensity.

  - Open door and pull the tray out then place sample on the center of the tray. Slide the tray back into the chamber.

  - Close the door.

  - To start the expose process, set the rocker switch to either Manual or Time. If using Time, set the timer to the desired exposure time then press the Actuate button.

  - If using Manual exposure, press the Actuate button until desired time is achieved then release the Actuate button to stop.

  - Remove sample from the chamber by sliding the tray out.

  - Turn the unit off by pressing the power button “OFF”.

# Text boxes

| SPECIFICATION FORMAT: |  |
| --- | --- |
| EQUIPMENT MANUFACTURER: | DYMAX |
| EQUIPMENT MODEL: | 38100 – 5000-EC |
| FDC ASSIGNED TOOL ID NUMBER: | A.S.U. Property # no tag |
| APPLICATION PROGRAM(S) AND REVISION: | Microsoft Word 2003 |