| FLEXIBLE DISPLAY CENTER | Document Owner: Nick Munizza | Release Date: |
| --- | --- | --- |
| Document Title: Pull Test / Adhesion Strength Operating Procedure for Jinlong | Document No: | Document Rev: 01 |

| SIGNATURES FOR RELEASE OR HISTORY ON FILE IN PRODUCT SPECIFICATIONS | Confidential Proprietary |
| --- | --- |
| ORIGINATOR: Nick Munizza | The information contained in this document is the property of the Flexible Display Center at Arizona State University. No information contained in this document may be disclosed outside of the Flexible Electronics and Display Center at Arizona State University at any time. |
| RESPONSIBLE ENGINEER: Emmett Howard |  |
| DIRECTOR OF OPERATIONS: |  |  |

Table of Contents

1.0	Purpose	3

2.0	Scope	3

3.0	Associated Materials and Equipment	3

4.0	Safety 	3

5.0	Procedures	3-4

6.0		Maintenance/ Engineering										4

# Purpose

  - To define the operating procedures for the Jinlong PEEL strength tester.

# Scope

  - Outline the procedure for measuring the adhesion strength of films.

- Associated Materials and Equipment

  - Sample for PEEL strength measurement.

- Safety

- Procedures

  - Log onto the computer.

  - On the desktop, double click the Blank Pull Test File.

  - A window will appear to select the com port. Select Com 1 and click OK.

  - Click DB1 Set up.

  - Select Fast Acquisition and click OK.

  - Be sure the sample tray is completely to the end (left of the rail).

  - Load sample onto the tray. Be sure the tab, is placed under the roller and the sample is sitting secure.

  - Secure the Tab to the adjustable clamp hanging from the meter.

  - Zero out the meter prior to attaching material to the clamp

  - Be sure to leave some slack on the tab.

  - Press the button located on top of the speed control box to start data collection.

  - Press Green UP button on the control panel.

  - Data collection on the sample will begin.

  - Once data collection has completed, press the stop button on front of the control panel to stop the PEEL process.

  - Press the button on top of the speed control box to stop data collection.

  - Wait until data collection has stopped collecting data before continuing.

  - Create a New folder with the lot ID of the sample.

  - Name each sample.

  - Repeat steps 5.3 to 5.20 until all samples are completed.

  - Close out the Blank Pull Test File.

  - Sign off on the computer.

- Maintenance/ Engineering

  - Notify engineering of any equipment issues.

  - Clean up area when you are finish.

# Text boxes

| SPECIFICATION FORMAT: |  |
| --- | --- |
| EQUIPMENT MANUFACTURER: | Jing Testing Machine Co., LTD |
| EQUIPMENT MODEL: | SG-L09 |
| FDC ASSIGNED TOOL ID NUMBER: | A.S.U. Property # None |
| APPLICATION PROGRAM(S) AND REVISION: | Microsoft Word 2003 |